## Slide 1
In Situ Irradiation of Spent Nuclear Fuels
Fuel and Cladding Materials
May 12, 2026
Cameron Howard
PIE Research Scientist

## Slide 2: Outline
Background & Motivation
In-situ TEM Re-Irradiation
  Fission Product Evolution
  Grain Evolution
Conclusions
Publications

## Slide 3: Background & Motivation

## Slide 4: Motivation
Enhance scientific understanding of mechanisms leading to high burnup structure (HBS).
Develop experimentally validated computational capabilities to predict microstructural evolution.
Increase allowable burnup limit of UO2 in commercial nuclear power plants.
62 GWd/MTU → 75-80 GWd/MTU
Longer reactor cycles/less refueling
Purchase fewer fuel assemblies
https://www.nrc.gov/reactors/power/atf/licensing-activities/licensing-actions.html#burnup
RIL 2021-13, “Interpretation of Research on Fuel Fragmentation, Relocation, and Dispersal (FFRD) at High Burnup.”

## Slide 5: UO2 High Burnup Structure
Dislocations accumulate and create large networks.
New defect free sub-grains form.
Intragranular fission gas concentration depletion.
Intergranular spherical fission gas bubbles.
92 MWd/kgU @ 1300 °C
55 MWd/kgU @ 450 °C
Sonoda, T., et al. "Transmission electron microscopy observation on irradiation-induced microstructural evolution in high burn-up UO2 disk fuel." Nuclear Instruments and Methods in Physics Research Section B: Beam Interactions with Materials and Atoms 191.1-4 (2002): 622-628.
Gerczak, Tyler J., et al. "Restructuring in high burnup UO2 studied using modern electron microscopy." Journal of Nuclear Materials 509 (2018): 245-259.
72 MWd/kgU
LAGB
HAGB
82 GWd/tHM
74 GWd/tHM
75 MWd/kgU @ 1000 °C
Spino, J. "Formation of the rim structure in high burnup fuel." Journal of Nuclear Materials 248 (1997): 170-179.
Rondinella, Vincenzo V., and Thierry Wiss. "The high burn-up structure in nuclear fuel." Materials today 13.12 (2010): 24-32.
72 MWd/kgU
66.6 GWd/thM
160 GWd/thM
75 GWd/thM
75 GWd/thM
Critical burnup ~60-70 GWd/thM
Fragmentation threshold
Capps, Nathan, et al. "A critical review of high burnup fuel fragmentation, relocation, and dispersal under loss-of-coolant accident conditions." Journal of Nuclear Materials 546 (2021): 152750.
Notes: Historically referred to as “rim” structure
Grain subdivision also referred to as restructuring

## Slide 6: Legacy BR3 UO2 Fuel
Well defined irradiation history & well studied
Intermediate rod averaged burnup: ~40 MWd/kgU
Some rim regions suggest early stage HBS formation
Electrolytic reduction for FP chemical analyses [i]
Grain subdivision and HR sub-grain structure maps [ii]
Original GBs
[i] S. Herrmann, S. Li, M. Simpson, “Electrolytic reduction of spent light water reactor fuel - Bench-scale experiment results”, J. Nucl. Sci. Technol., 44 (2007) 361–367.
[ii] R. Yuan, J. Zhang, L. He, J. Zuo, “Training artificial neural networks for precision orientation and strain mapping using 4D electron diffraction datasets”, Ultramicroscopy, 231, 2021, 113256.
Drive BR3 UO2 fuel to fully evolved HBS in-situ at temperature
+ irradiation
IVEM in-situ TEM re-irradiation at ANL
+ stress
in-situ compression & creep testing at INL
What are the contributing mechanisms to HBS?
How can we simulate them and perform separate effects studies?
Notes: What are the contributing mechanisms to HBS? How can we simulate them and perform separate effects studies?

## Slide 7: In-Situ TEM Re-Irradiation

## Slide 8: Sample Preparation
5 FIB lift outs taken from remaining volume of Block C after slice and view performed at regions where sub-grain structure observed in BSE image.
L1
L2
L4
L5
L3
Additional FIB lift outs taken from bulk at R ~ 0.9 adjacent
to cube lift out locations.
r/r0 ≈ 0.99
r/r0 ≈ 0.87

## Slide 9: Irradiation Conditions
2+
+
+0.16% FIMA
+0.65% FIMA
Notes: More Xe ion deposition in TEM lamellas compared to Kr ion deposition.

## Slide 10: Fission Product Evolution

## Slide 11: 1 MeV Kr2+ Irradiation
Temperature
Added Dose
0 dpa
0.32 dpa
3.24 dpa
1.62 dpa
RT
300 °C
0 dpa
0.31 dpa
1.54 dpa
3.08 dpa
500°C
0 dpa
0.35 dpa
1.74 dpa
3.48 dpa
Notes: -0.75 µm to -1.5 µm underfocus/overfocus for bubble/pair measurements

## Slide 12: 1 MeV Kr2+ EDS
Before Re-Irradiation
After Re-Irradiation @ 300 °C to 3.08 dpa
1. Faster diffusion rate of 5MPs compared to Xe
2. Less uniform distributions/spacings
3. Size reductions
4. Number density reductions
Notes: Note: Mo grids used for robustness in HT irradiation set up, so Mo signal is obscured by Mo background signal from grid. Diamond TEM grids are a lot more expensive, would be useful for differentiating Mo.

## Slide 13: 1 MeV Kr2+ Irradiation: Bubble and Pair Size Reductions

## Slide 14: 1 MeV Kr2+ Irradiation: Pair Density Depletion

## Slide 15: 300 keV Xe+ Irradiation
Temperature
Added Dose
RT
300 °C
0 dpa
1.47 dpa
5.89 dpa
2.95 dpa
0 dpa
1.61 dpa
6.44 dpa
3.22 dpa
-223 °C
(high flux)
0 dpa
0.34 dpa
3.43 dpa
1.71 dpa
17.16 dpa

## Slide 16: 300 keV Xe+ Irradiation: Bubble and Pair Size Reductions

## Slide 17: 300 keV Xe+ Irradiation: Pair Density Depletion

## Slide 18: Metallic Precipitates Re-Precipitation
2.34 dpa
2.39 dpa
2.44 dpa
2.53 dpa
3.23 dpa
4.10 dpa
4.99 dpa
5.86 dpa

## Slide 19: Pair Dissolution to 5MP Re-Precipitation Graphic
Starting microstructure
-Initial size reductions
-Xe ions:
1) Trapped in matrix V
2) Attach to pairs
3) Bind w/ detached Xe/Kr atom
-Detached Xe/Kr atoms:
1) Form bubbles
2) Dissolve into matrix
3) Annihilate at IG pores
4) Escape at free surface
-5MPs: Uniformly redistribute in matrix to supersaturation
point.
-Close spacing: Re-precipitation of 5MPs via backflow diffusion to existing clusters.
-Large spacing: Continuous dissolution
-Nucleation of new Xe/Kr gas bubbles from implanted ions.
Agrees w/ Nelson, Hudson, and Mazey (NHM) model

## Slide 20: Grain Evolution

## Slide 21: 300 keV Xe+ Re-Irradiation at -223 °C
High Flux:
Low Flux:
Minimal grain evolution: little to no grain growth, ion sputtering opens pore
0 dpa
Added Dose
1.71 dpa
3.43 dpa
17.16 dpa
0 dpa
1.17 dpa
2.34 dpa
11.72 dpa

## Slide 22: High Density of 5MPs near pore restricts GB Migration at -223 °C
After 11.72 dpa of added damage

## Slide 23: 300 keV Xe+ Re-Irradiation at RT
0 dpa
0.88 dpa
2.95 dpa
11.78 dpa
14.73 dpa
Added Dose
Most nanograins grow and merge into bigger adjacent grains

## Slide 24: 300 keV Xe+ Re-Irradiation at 300 °C
0 dpa
6.44 dpa
16.1 dpa
Arrows indicate nanograin growth and merger into larger grain.
Notes: Rings become fainter and disappear transitioning to more distinct spots also indicating grain growth

## Slide 25: Grain Size Evolution vs. Dose, Temperature and Initial Grain Size
Thermal activation required for growth
Grains < 30 nm: population decrease
Grains > 30 nm: population increase

## Slide 26: Critical Transition Grain Size from Growth to Subdivision
200-900 nm
Notes: Critical size suspected to be smaller for TEM lamellas compared to bulk irradiations due to increased free surface area to volume causing increased defect annihilation at the surfaces

## Slide 27: Conclusions: Fission Product Evolution
  Over the complete range of temperatures (-223-500 °C) with both Kr2+ and Xe+ ions:
    Number density of fission gas bubble-5 metal precipitate pair structures decreases.
      Completely vanish at high dose: +9 dpa @ RT, +13 dpa @ 300 °C
    Sizes of pre-existing fission gas bubbles and metallic precipitates reduced.
      Faster diffusion rates of 5MPs vs. fission gases
    Increasing ion flux accelerates the reduction.
    Re-precipitation of metallic precipitates was also observed in real time video imaging.
    High dose implants new sub-nm Xe bubbles.
  Supports fission gas re-solution & precipitate re-precipitation/dissolution mechanisms (NHM model).
    Atomic diffusion coefficient has strong irradiation dependence but weak temperature dependence.
Notes: TEM: fission gas re-solution & precipitate dissolution

## Slide 28: Conclusions: Grain Evolution
Nanograin growth during ion irradiation in-situ in the TEM.
  Severe: 300 °C
  Moderate: RT
  Negligible: -223 °C
Thermal activation requirement to overcome GB pinning by fission gas bubbles, precipitates, and pores.
Largest grains (> 300 nm) do not grow or subdivide.
  Free surface defect annihilation contributions
  Limited 300 keV Xe+ ion electronic stopping power

## Slide 29: Publications
Sakib, Sadman, Yunyuan Lu, Cameron B. Howard, Jatuporn Burns, Wei-Ying Chen, Linu Malakkal, Chao Jiang, Sudipta Biswas, Fabiola Cappia, and Lingfeng He. "In-situ ion irradiation of fission products in a spent UO2 fuel." Journal of Nuclear Materials 614 (2025): 155859.
Sakib, Sadman, Yunyuan Lu, Cameron B. Howard, Jatuporn Burns, Mario Matos, Wei-Ying Chen, Sudipta Biswas, Fabiola Cappia, and Lingfeng He. "In-situ ion irradiation induced nanograin growth in a spent UO2 fuel." Journal of Nuclear Materials (2025): 156394.