## Slide 1: The Post Irradiation Examination Ion-bombarded High-entropy Carbide Ceramics
Todd Sherman ISU–NSUF 2026

## Slide 2: Overview
Project background
NSUF – Post Irradiation Examinations
X-ray Diffraction (XRD)
Electron backscatter diffraction (EBSD)
Nanoindentation hardness testing
TEM
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM

## Slide 3: Project Background
New series of high-entropy carbide ceramics
Synthesis parameters and material characterization
Mechanical and thermodynamic characterization
Analytical radiation shielding applicability
Heavy ion bombardment
Post Irradiation Examination (PIE)
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM

## Slide 4: Synthesis
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Six equimolar 5-principal element high entropy-based combinations from mono carbide powers
TiC, VC, ZrC, NbC, TaC & WC
  Material 1 - (Ti V Zr Ta W)C
  Material 2 - (Ti V Zr Nb W)C
  Material 3 - (Ti V Zr Nb Ta)C
  Material 4 - (Ti V Ta Nb W)C
  Material 5 - (Ti Zr Nb Ta W)C
  Material 6 - (V Zr Nb Ta W)C
High energy balling → Spark Plasma Sintering

## Slide 5: Material Characterization
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Density
X-ray Diffraction (XRD)
Nanoindentation hardness testing
Thermal Diffusivity and Conductivity
Chart: (TiVZrTaW)C

## Slide 6: Radiation Shielding Analysis & Heavy Ion Bombardment
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Analytical radiation shielding evaluations for photon and neutron shielding applications
10 MeV Au-ion irradiation
Fluence 1 = 1.3 x 1016 ion/cm2 → 43-47 dpa
Fluence 2 = 2.6 x 1016 ion/cm2 → 85-95 dpa
Chart: 2.6x1016 ion/cm2 10 MeV Au-ions in (TiVZrTaW)C
Shielded region
Polished surface

## Slide 7: Post Irradiation Examinations XRD
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Comparison of X-ray Diffraction (XRD) plots of the unirradiated and the two irradiated surfaces
Chart: 2θ (degrees)
Formation of an unknown phase at highest fluence

## Slide 8: Post Irradiation Examinations EDS
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Energy Dispersive X-ray Spectroscopy (EDS)
Zr clustering

## Slide 9: Post Irradiation Examinations EBSD
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Electron Backscatter Diffraction (EBSD)
Chart: Grain Size Distribution
| 0.94476400000000005 | 1.0621799999999999 | 1.19418 | 1.34259 | 1.5094399999999999 | 1.69703 | 1.9079299999999999 | 2.1450399999999998 | 2.4116200000000001 | 2.7113299999999998 | 3.0482900000000002 | 3.4271199999999999 | 3.85303 | 4.3318700000000003 | 4.8702199999999998 | 5.4754699999999996 | 6.1559499999999998 | 6.9209899999999998 | 7.78111 | 8.7481200000000001
Unirradiated | 0.069542 | 0.044014 | 0.06338 | 0.047535 | 0.058099 | 0.070422 | 0.089789 | 0.081866 | 0.091549 | 0.088028 | 0.075704 | 0.073063 | 0.058099 | 0.034331 | 0.03081 | 0.0096831 | 0.0088028 | 0.0026409 | 0.0017606 | 0.00088028
1.3e10^16 | 0.080842 | 0.086773 | 0.09745 | 0.083215 | 0.093891 | 0.10931 | 0.10931 | 0.14015 | 0.14134 | 0.13422 | 0.14015 | 0.13304 | 0.11999 | 0.10219 | 0.10694 | 0.082029 | 0.06898 | 0.060676 | 0.055931 | 0.053559
2.6e10^16 | 0.12091 | 0.14878 | 0.12875 | 0.1331 | 0.17143 | 0.15662 | 0.16533 | 0.18972 | 0.18275 | 0.19233 | 0.20801 | 0.18101 | 0.18275 | 0.15923 | 0.14094 | 0.12439 | 0.10784 | 0.10348 | 0.10174 | 0.10087

## Slide 10: Post Irradiation Examinations Nanoindentation
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Chart: Hardness [GPa]
| Unirradiated
Unirradiated | 23.76
Irradiated 1.3E16 | 23.06
Irradiated 2.6E16 | 31.26
Chart: Depth [nm]

## Slide 11: Post Irradiation Examinations TEM
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Transmission Electron Microscope (TEM)

## Slide 12: Post Irradiation Examinations TEM
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Amorphization vs irradiation depth

## Slide 13: Post Irradiation Examinations TEM
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Secondary ZrO2 phase identification
Element Weight % Atomic % Uncert. %
------- -------- -------- ---------
O(K) 29.39 70.36 1.09
Zr(K) 70.60 29.63 1.72
Element Weight % Atomic % Uncert. %
------- -------- -------- ---------
Ti(K) 7.84 21.58 0.26
V(K) 6.43 16.64 0.25
Ta(L) 27.73 20.19 0.68
W(L) 57.98 41.56 0.96

## Slide 14: Post Irradiation Examinations TEM
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Grain Boundary Segregation

## Slide 15: Questions?
OVERVIEW
PROJECT BACKGROUND
NSUF-PIE
XRD
EDS
EBSD
NANOINDENTATION
TEM
Todd Sherman
toddsherman@isu.edu
todd.sherman@inl.gov