## Slide 1
Irradiation Testing and Experiment Design
ATR capsules and loops | TREAT transient testing
July 22, 2026
Nate Oldham
Experiment Design Engineering Manager

## Slide 2
Table of Contents
ACT | SLIDES | PURPOSE
1 | 1–5 | TYPES OF IRRADIATION TESTS + DESIGN DECISION LOGIC
2 | 6–9 | FACILITY + ARCHITECTURE ¦ ATR and TREAT
3 | 10–18 | CAPSULES ¦ Type of Irradiation Vehicle
4 | 17-18 | INSTRUMENTATION LEADOUT ¦ Type of Irradiation Vehicle.
5 | 19–23 | PRESSURIZED-WATER LOOP ¦ Type of Irradiation Vehicle.
6 | 24–26 | TREAT TRANSIENT TESTING ¦ Type of Irradiation Vehicle.
7 | 27 | CLOSE + QUESTIONS

## Slide 3: Think in test campaigns, not single irradiations
Each facility answers a different part of the technical question.
ATR DROP-IN CAPSULE
Screen concepts
Accumulate dose or burnup
Compare materials and specimens
ATR INSTRUMENTED / LOOP
Control key conditions
Measure selected responses
Increase environmental fidelity
TREAT TRANSIENT
Apply controlled rapid energy input
Capture time-resolved response
Explore thresholds and progression
PIE + models + fabrication records + facility history = the defensible dataset

## Slide 4: Start with the decision, not the hardware
A good experiment concept is a traceable chain from the decision to the data product.
1 Research question
What decision will the test support?
2 Measured response
What observable changes that decision?
3 Success criterion
What result is sufficient or unacceptable?
4 Environment + history
Spectrum, dose, temperature, chemistry and time.
5 Architecture + controls
Capsule, lead, loop or transient vehicle.
6 PIE + data pedigree
How will evidence be recovered and defended?
If one link is vague, the hardware will not make the result defensible.

## Slide 5: ATR and TREAT answer different parts of the LWR question
ATR | STEADY-STATE IRRADIATION
TREAT | TRANSIENT IRRADIATION
Dose, burnup, and microstructure evolution
Temperature and environment over time
Capsule, instrumented, and water loop configurations
Rapid power or energy deposition
Time-resolved response and diagnostics
Transient vehicle, confinement, and recovery
Connect histories

## Slide 6: ATR at a glance
Materials and fuels test reactor with multiple experiment positions
Pressurized light-water primary coolant and downflow through the core
Cloverleaf core supports different flux conditions in the same cycle
Position selection affects spectrum, heating, space and interfaces
Cycle history and control configuration become part of the test record

## Slide 7: ATR position and experiment types
DROP-IN CAPSULE
Passive hardware in an available reactor position; containment and thermal gaps do most of the work.
INSTRUMENTED LEAD
Leadouts connect sensors and sweep-gas controls to external systems.
PRESSURIZED WATER LOOP
An independent coolant system provides pressure, temperature, flow, and chemistry control.
Diameter + flux + spectrum + heating + handling + interfaces

## Slide 8: TREAT at a glance
Uranium-fueled, graphite-moderated, once-through air-cooled thermal-spectrum test reactor
Fast-acting rods produce natural bursts or shaped power histories
Strong negative temperature feedback makes excursions self-limiting
Central test positions support pins, clusters and specialized experiment vehicles
Open-core access enables time-resolved diagnostics, including the fast-neutron hodoscope
PEAK TRANSIENT POWER
up to ~18 GW
core dependent
TYPICAL TRANSIENT DURATION
tens of msec to a few sec
some shaped cases last minutes

## Slide 9: Choose the simplest architecture that meets the objective
Architecture is a trade space: choose by decision, fidelity, control strategy and time scale.
Decision factor | Drop-in capsule | Instrumented lead | Pressurized loop | Instrumented TREAT vehicle
Best fit | Screening / accumulation | Controlled exposure | Qualification-oriented evidence | Transient thresholds / progression
Environment | ATR primary boundary outside capsule | ATR position + local gas control | Independent PWR-like coolant | Vehicle-defined capsule or loop boundary
Real-time data | Usually none | Selected sensors | Sensors + loop-system data | Many high-speed sensors + facility diagnostics
Control strategy | Passive geometry / gas gap | Sweep gas + feedback | Coolant system + local design | Dedicated experiment controls / DAQ synchronized with reactor transient
Integration effort | Lowest | Intermediate | Highest | High; fast timing + recovery interfaces
Use when... | The decision tolerates lower fidelity | Real-time control changes the answer | Coolant fidelity changes the answer | Time-resolved response changes the answer

## Slide 10: Drop-in capsule testing
ATF-1 illustrates how modular containment supports early LWR fuel screening.
CONTAIN
POSITION
CONTROL TEMPERATURE

## Slide 11: ATF-1: screen LWR fuel concepts efficiently
Fuel and cladding concepts are enclosed in individual capsules
Steady-state irradiation is followed by post-irradiation examination
A common facility position supports comparative evidence
Containment enables early concepts to be tested with defined boundaries
The decision is which concepts merit more prototypic testing
Concept
Capsule
ATR exposure
PIE
Down-select

## Slide 12: The small-I basket makes capsule testing modular
HISTORICAL CONFIGURATION
4 locations x 3 channels x 7 axial locations = 84 capsule positions
DESIGN IMPLICATION
Specimen identity, axial location, flux monitoring, handling and PIE retrieval must remain traceable.

## Slide 13: Capsule anatomy controls containment and specimen temperature
Capsule boundary separates the specimen from ATR primary coolant
Holder geometry locates the rodlet and maintains handling features
The gas gap creates thermal resistance and elevates cladding temperature
Materials, dimensions and tolerances set the heat-transfer path
Closures, inspection and PIE access are part of the same design
  ATR Top View

## Slide 14: Drop-in capsules are powerful when their limits match the decision
STRENGTHS
Modular and reconfigurable
High position capacity
Established fabrication methods
Individual containment boundaries
Good first in-reactor test for new concepts
LIMITS
Lower environmental fidelity
Usually no real-time instrumentation
Passive temperature control
Local flux and heating constraints
High-heat concepts can be difficult to keep in range
Use a capsule when screening value exceeds the value of added fidelity and instrumentation.

## Slide 15: Thermal design connects nuclear heating to specimen temperature
Neutronics predicts local heat generation and uncertainty
Geometry and materials establish conduction paths
Gas composition and gap size establish thermal resistance
Radiation, contact and surface conditions can matter
Coolant boundary conditions close the thermal model
UNCERTAINTY BUDGET
Heat-rate uncertainty, power variation, gap tolerances, properties and model assumptions can all move the result.

## Slide 16: Select temperature evidence that matches the decision
Method | What it tells you | Design question
Melt wire | Peak threshold exceeded | Is one threshold sufficient?
SiC indicator | Post-irradiation inference | Is the method calibrated for the range?
Thermocouple | Real-time temperature history | Will routing, drift and survival be acceptable?
Post-irradiation access and chain of custody are part of the measurement system.

## Slide 17: Instrumented capsules add control and real-time evidence
Leadouts connect in-core sensors and sweep-gas lines to external systems
Gas mixing can adjust conductance and specimen temperature
Selected thermocouples provide control feedback and operating history
Exhaust monitoring can add experiment-performance information
Every line creates routing, sealing, calibration and survivability requirements
Use instrumentation when the information gained justifies the added failure modes and integration work.

## Slide 18: AGR shows how requirements become a complete test train
The research objective drives capsule zoning, specimen placement and instrumentation
Individual capsule functions must integrate with the full test-train structure
Lead routing, handling, assembly and qualification are system-level decisions
The final dataset connects in-reactor history to post-irradiation fuel performance
TRISO fuel form
Particle cross sections

## Slide 19: Pressurized-water loop testing
ATF-2 illustrates prototypic coolant conditions and tighter facility integration.
PRESSURE + TEMPERATURE
FLOW + CHEMISTRY
TEST-TRAIN INTEGRATION

## Slide 20: The loop and test train form one experiment system
Loop coolant is isolated from ATR primary coolant
Dedicated systems control pressure, temperature, flow and chemistry
The in-pile tube, test train and external plant share interfaces
Facility transients and operating procedures enter the design basis
Use a loop when coolant fidelity changes the technical decision
SOURCE EXAMPLE: ~15 MPa | ~300 C

## Slide 21: ATF-2 moves mature LWR concepts into PWR-like conditions
The test train occupies the center flux-trap loop position
Fuel pins contact the independent loop coolant directly
Pressure, temperature, flow and chemistry are controlled as a system
Local power depends on core position and control configuration
The loop supports evidence closer to qualification needs
DESIGN CONSEQUENCE
Core-physics variability must be carried into tier design, power history and uncertainty.

## Slide 22: Five tiers turn irradiation requirements into a test train
TIERING
Five axial tiers place specimens at different locations in the flux profile.
SHROUDING
Local material and geometry tailor power to the target condition.
HOLDERS
Each holder locates six rodlets and supports vertical reconfiguration.

## Slide 23: Instrumentation multiplies the integration interfaces
Thermocouples measure selected fuel or holder temperatures
Displacement sensors add routing, calibration, and range requirements
Each connector and feedthrough must survive fabrication and operation
Non-fueled testing can qualify the integrated measurement chain
Test-train wiring must coexist with reactor-top handling and operations
REACTOR-TOP INTERFACE
Connector access, routing, strain relief, handling, and configuration control.
Qualification is for the complete measurement path, not only the sensor.

## Slide 24: Transient testing in TREAT
The design emphasis shifts from accumulated exposure to energy deposition, time response and recoverable evidence.
DEFINE THE TRANSIENT
CAPTURE THE RESPONSE
RECOVER THE EVIDENCE

## Slide 25: Transient tests change the dominant design questions
INPUT
What transient shape, timing and deposited energy represent the event of interest?
VEHICLE
What geometry, thermal boundary and confinement preserve the intended response?
DIAGNOSTICS
Which signals require high time resolution, calibration and protection from the event?
RECOVERY
What must remain identifiable and examinable after the transient?
The experiment vehicle must preserve both the physics and the evidence.

## Slide 26: TWIST Device
Most components remain unchanged from previous TWIST experiments
  Capsule will be configured with an external borated steel flux collar like previous RIA tests
Only changes are modifications to the rodlet holder and the addition of heaters to get to the desired pre-transient conditions
Borated stainless steel Flux Collar on TWIST capsules used for RIA testing