## Slide 1
Automated Regions of Interest (ROI) Detection in Irradiated U-Zr Metallic Fuel Using Deep Learning Method
By Tiankai Yao
Prepared for NSUF Annual Program Review
04/17/2025

## Slide 2: Nuclear Fuel Post Irradiation Examination
Photo observation of U-10Zr fuel pins irradiated in Fast Flux Test Facility (~1 m)
OM examination (U-10Zr fuel) (1mm, 10-3 m )
Scanning electron microscopy characterization
of U-10Zr grain and precipitate (1 μm, 10-6 m)
INL PIE capabilities span 10 orders of magnitude
Atom probe tomography study of Zr atom distribution in 3D
(3 Å, 10-10 m)
50 µm
2 µm
Transmission electron microscopy identification of Zr nano precipitate (2-5 nm, 10-9 m)
2 µm
500 nm
U
Zr

## Slide 3: ROI is the starting point of materials characterization

## Slide 4: ROI and Image Analysis
Is the ROI selected representative of irradiated fuel
If Yes, proof?
If not, how to make sure it is representative
Automation
Efficiency
Cost

## Slide 5: 10, 000 images stitched to cover the whole area

## Slide 6: Deep learning

## Slide 7: Singe-phase vs two-phase
Comparison of single-phase and two-phase training. The top row shows annotated ROIs, serving as ground truth. The middle row shows ROI proposals inferred using the single-phase model, while the bottom row shows ROI proposals generated by the two-phase model, highlighting its performance. Sth represents the prediction threshold score.

## Slide 8: 2nd phase with modified weight loss function
The top row shows annotated ROIs. The middle row shows ROI proposals inferred using the two-phase model utilizing original loss functions, while the bottom row shows ROI proposals generated by the two-phase model with modified weighted loss functions. Sth represents the prediction threshold score.

## Slide 9: Compared with other methods in literature
Visual comparison of ROI proposals generated by two variations of RetinaNet and our Proposed Method.

## Slide 10: Compared with Faster RCNN method

## Slide 11: Model Performance by Numbers

## Slide 12: Other AI models developed and deployed on NSUF NRDS site

## Slide 13: Other AI models developed and deployed on NSUF NRDS site
Accurate Segmentation of Localized Corrosion in Structural Alloys via Deep Learning

## Slide 14: Performance comparison
Without (c) and with (d) texture refinement

## Slide 15: Thank you