## Slide 1: In-situ Irradiation of Uranium Carbide and Zirconium Carbide
1North Carolina State University
2Idaho National Laboratory
3Argonne National Laboratory
4University of Michigan
Rashed Almasri1; Adrian Wagner2; Laura Hawkins2; Wei-Ying Chen3; Yuhan Li4; Jian Gan2 ; Lingfeng He1
4-16-2025
The 2025 NSUF Annual Program Review

## Slide 2
Introduction
UC as a Promising Nuclear Fuel
Historical Context: Developed in mid-20th century for NASA’s NERVA program; valued for high thermal conductivity and uranium density. Later explored for molten salt/sodium-cooled fast reactors.
Shift to UO₂: UO₂ became industry standard due to stability and compatibility with light water reactors (LWRs).
Resurgence in Advanced Reactors: UC regains attention for Generation IV systems (e.g., gas-cooled fast reactors, VHTRs) and TRISO fuels (e.g., UCO kernels).
Placement of various advanced reactor concepts on scales describing the ranges of values of components of the environment for core materials1
1G. Was, et al. 2019

## Slide 3
Introduction
Superior Properties: Higher uranium density (12.9 vs. 9.7 g/cm³) and thermal conductivity (22 vs. 3 W/m·K at 1200 K).
Design Benefits: Enables compact cores, reduces thermal gradients, and mitigates melting risks.
Material Compatibility: Stable with SiC/ZrC cladding (e.g., proposed in General Atomics’ EM2 reactor).
Advantages of UC over UO₂
The crystal structure of UC1
1University of Liverpool. (2024). ChemTube3D.

## Slide 4
Introduction
Knowledge Gap & Study Focus
Irradiation Performance: Limited data on UC’s response to radiation (swelling, defect formation).
Research Approach: In situ TEM analysis of radiation-induced defects (Xe/Kr ion irradiation) and swelling.
Comparison with UO₂: Contrasts UC’s dynamic microstructural evolution with well-documented UO₂ behavior.

## Slide 5
Introduction
High Melting Temperature: 3420 oC, part of UHTCs (ultra-high temperature ceramics)1.
Thermal & Electrical Conductivities: Higher than other materials.
Mechanical Properties: Excellent strength and durability.
Resistance & Absorption: Resistant to fission products and low neutron absorption cross-section.
It can be used as:
  Inert fuel matrix for GFRs2
  Oxygen-getter for microencapsulated fuels3
  Cladding alternative for advanced reactors4
  Fission product barrier in TRISO fuel particles5
Zirconium Carbide (ZrC)
1I. L. Shabalin, 2019.
2G. Vasudevamurthy et al., 2008.
3D. Wongsawaeng, 2010.
4K. A. Terrani, 2018.
5I. E. Porter, et al., 2018.

## Slide 6: Experimental
Synthesis:
  Single-phase UC synthesized and sintered at Idaho National Laboratory (INL).
Purity Validation:
  XRD analysis confirms high-purity UC.
Microstructure Characterization:
  Optical microscopy reveals a high-density as-sintered pellet with equiaxed grains (10s to >100 µm in size).
TEM Sample Preparation:
  TEM lamellas prepared via the Focused Ion Beam (FIB) technique (FEI Quanta 3D FIB).
  Mounted on molybdenum (Mo) grids at INL’s Irradiated Materials Characterization Laboratory (IMCL).
Sample Preparation

## Slide 7: Experimental
In-Situ Ion Irradiation:
  Conducted using the Intermediate Voltage Electron Microscope (IVEM) at Argonne National Laboratory (ANL)
Microstructural Evolution Analysis:
  In-situ TEM images captured at multiple irradiation doses.
  Manual quantification of dislocation loops and Xe bubbles:
    Diameters measured individually.
    Densities calculated using ImageJ software1.
Ion | Temperature °C | Final Dose ions/cm2
1 MeV Kr2+ | 300 | 9.38 × 1014
 | 600 | 
300 keV Xe+ | 300 | 2.5 × 1015
 | 600 | 
 | 900 | 
1M.D. Abràmoff, et al., 2004.
Kr++/Xe+
e- beam

## Slide 8: Experimental
Sample Thickness Measurement:
  Electron Energy Loss Spectroscopy (EELS) applied to determine sample thickness1.
Advanced Characterization:
  Elemental distribution analyzed via 200 kV FEI Titan TEM equipped with ChemiSTEM™ technology.
SRIM Simulations:
  Simulated depth profiles and atomic displacements using Kinchin-Pease mode:
Chart: Thickness (nm)
Kr++
Chart: Thickness (nm)
Xe+
1T. Malis, et al., 1988

## Slide 9: Results
Xe bubble formation at a) 600 oC under-focus and b) over-focus and at c) 900 oC under-focus and d) overfocus, all by 1 micron.
Dose (dpa) | Temp (°C) | Swell (%) | Average Size (nm)
9.3 | 600 | 0.36 | 1.14±0.26
9.3 | 900 | 0.6 | 1.34±0.39
While there is expected to be an increase in bubble sizes and swelling at higher temperatures, our samples showed only marginal changes.

## Slide 10: Results
TEM BF images in the two-beam condition showing the formation and evolution of dislocation loops about irradiation temperature and dose in the Kr irradiated samples.

## Slide 11: Results
Chart: Dose (x1014 ions/cm2)
| 0 | 3.13 | 6.25 | 9.3800000000000008
300 °C | 2.4693 | 6.3832 | 6.3623 | 7.0437
600 °C | 1.8066 | 3.9433 | 1.5375 | 1.3758
Chart: Dose (x1014 ions/cm2)
| 0 | 3.13 | 6.25 | 9.3800000000000008
300 °C | 3.8559 | 8.0998 | 9.2409 | 10.9964
600 °C | 5.4752 | 9.2478 | 19.4671 | 20.6908
Dislocation loop density concerning irradiation dose
Dislocation loop size evolution with the irradiation dose

## Slide 12: Results
Dislocation loop size frequency depending on the dose at 300 oC and 600 oC.

## Slide 13: Results
Dislocation loop size frequency depending on the dose at 300 oC and 600 oC.

## Slide 14: Results
Dislocation loop size frequency depending on the dose at 300 oC and 600 oC.

## Slide 15: Results
Dislocation loop size frequency depending on the dose at 300 oC and 600 oC.

## Slide 16: Results
Nanograin-like structure appears at thin regions after irradiation.

## Slide 17: Results
EDS maps and spectrum for the nano-grained microstructure observed in UC irradiated at 600 oC
U - K

## Slide 18: Discussion
Swelling data from other studies 1,2,3 compared to this work
Xe Bubble Formation & Swelling Behavior in Fuels
Bubble Size vs. Temperature:
  300 oC: Bubbles too small for TEM detection.
  600 oC & 900 oC: Smaller bubbles vs. oxide fuels4.
Swelling Measurements Comparison:
  Carbide/nitride fuels: Early TEM (nano-bubbles) + optical imaging (larger bubbles).
  Swelling values slightly higher in literature but show slow rise until critical temperature (900–1150°C), then sharp increase.
Critical Temperature:
  Matches onset of extensive grain growth.
  Carbide fuels: Lower bubble concentration due to higher carbon self-diffusivity5.
1C. Ronchi, et al., 1978.
2C. Ronchi, et al., 1975.
3H. Blank, et al., 1975.
4K. L. He, et al., 2015.
5H. Matzke, et al., 1977.

## Slide 19: Discussion
Chart: Dose (x 1014 ions/cm2)
| 0 | 3.13 | 6.25 | 9.3800000000000008
UC at 300°C | 3.8559 | 8.0998 | 9.2409 | 10.9964
UO2 at 600°C | 3 | 5 | 5.5 | 7.5 | 8.5
UC at 600°C | 5.4752 | 9.2478 | 19.4671 | 20.6908
UO2 at 800°C | 6.5 | 9.5 | 11.25 | 16.25 | 17
x axis | 0 | 0 | 0 | 0 | 0
Chart: Dose (x 1014 ions/cm2)
| 0 | 3.13 | 6.25 | 9.3800000000000008
UC at 300°C | 3.8559 | 8.0998 | 9.2409 | 10.9964
UC at 600°C | 5.4752 | 9.2478 | 19.4671 | 20.6908
UN at 700°C | 5.3 | 6.34 | 7.9 | 10 | 5.77 | 13.8 | 24.1
UN at 800°C | 7.11 | 9.05 | 10.4 | 10.9 | 14.1
x axis | 0 | 0 | 0 | 0 | 0
Dislocation loop size comparison with UO21
Dislocation loop size comparison UN2
1M. Kosmidou et al., 2025.
2L. F. He et al., 2013.

## Slide 20
Zirconium Carbide
Damage profiles and ion implantation modeled using the Kinchin-Pease model in SRIM.
Final Kr-irradiation dose: 1.8 dpa with 0.0052% Kr implantation in ZrC.
Final Xe-irradiation dose: 57 dpa with 2.4% Xe implantation in ZrC.
Kr++
Xe+

## Slide 21
Dislocation loops in ZrC at 800ºC (left) and 1000ºC (right) at 1.8 dpa.
Zirconium Carbide

## Slide 22
a) dislocation loop density and b) dislocation loop size analysis for ZrC irradiated up to 1.8 dpa at 800 oC and 1000 oC.
Zirconium Carbide

## Slide 23
a
b
Xe bubble formation in a) ZrC under-focus and b) over-focus, with a defocusing of 1 microns.
 | T (oC) | Dose (dpa) | Average Size (nm) | Swell (%)
ZrC | 800 | 57 | 3.4 | 0.6
UC | 600 | 9.3 | 1.1 | 0.4
 | 900 | 9.3 | 1.3 | 0.6
Size measurements of bubble and swelling for ZrC at 57 dpa and compared to UC.
ZrC showed very similar behavior to UC but at different doses, hinting that carbides might have similar swelling behavior.
Zirconium Carbide

## Slide 24
UC has shown a much higher dislocation loop density compared to ZrC.
This can be due to a difference in stoichiometry or a difference in interstitial diffusivity in the crystal lattice
Zirconium Carbide

## Slide 25
Dislocation loop size comparison for ZrC at 800 and 1000 oC, UC at 300 and 600 oC and ZrC at 600 and 800 oC [1].
ZrC shows smaller dislocation loops compared to UC.
ZrC has high energy barriers to both the zirconium and carbon migration.
Additionally, ZrC is stable in single phase at the sub-stoichiometric ZrC1-x which leaves a high concentration of carbon vacancies in the lattice that will combine with interstitials.
1C.J. Ulmer, et al., 2004.
Zirconium Carbide

## Slide 26
Expand irradiation studies to higher temperatures/doses.
Probe nano-grain origins and implications for fuel performance
Future Work
Conclusions
Limited Xe bubble growth/mobility observed; temperature is the dominant factor.
Critical swelling temperature likely higher than tested range; future high-temperature experiments needed.
Xe Ion Irradiation (≤900°C)
Dislocation loops formed similarly to oxide fuels.
Temperature (vs. dose) dominates loop growth:
  Peak loop density at 3 dpa (300°C) vs. 1 dpa (600°C).
Requires higher dose/temperature studies for mechanistic clarity.
Kr Ion Irradiation
Observed in thin irradiated regions; parallels seen in ZrC (outward deformation) and UO₂ (polygonization).
Formation mechanisms require targeted investigation.
Nano-grain Structures
Dislocation loop evolution in ZrC agreed with literature at lower temperatures.
ZrC exhibited microcracking, suggesting susceptibility to brittle fracture or stress accumulation under irradiation.
ZrC Irradiation

## Slide 27: Acknowledgements
This work was supported by the U.S. Department of Energy, Office of Nuclear Energy under DOE Idaho Operations Office Contract DE-AC07-05ID14517 as part of Nuclear Science User Facilities awards #4721 & #4892.
This work was possible with the collaboration and hard work of everyone at NCSU, INL and ANL

## Slide 28
Materials
In
eXtremes
MIX Lab
Y. Bao, L. He et al. J. Materiomics 5(2019) 657-662
Y. Zhou, L. He et al. J. Eur. Ceram. Soc. 33 (2014) 2831-2865
L. He et al. Acta Mater. 208 (2021)116778
L. He et al. J. Am. Ceram. Soc. 105 (2022) 5419-5435
Y. Wang, L. He et al. Mater. Sci. Eng. A 849 (2022) 143475
L. He et al. Mater. Lett.117 (2014) 120-123
Japanese Patent No. 5704640, 2015
K. Bawane, L. He et al. Scripta Mater. 197 (2021) 113790
https://www.ne.ncsu.edu/mix/

## Slide 29
Phase Diagrams