## Slide 1
Irradiation performance of Uranium Mononitride
Maria Kosmidou, Adrien E. Terricabras, Caitlin A. Kohnert, Joshua T. White, Erofili Kardoulaki
Contributors: Christopher Matthews, Hi T. Vo, Michael W.D. Cooper, A. David R. Andersson, Darrin D. Byler, Materials Science & Technology Division, Los Alamos National Laboratory
Collaborators: Wei-Ying Chen
Nuclear Science and Engineering Division, Argonne National Laboratory
Wednesday, April 16, 2025
NSUF Annual Meeting 2025
LA-UR-25-23399 | 

## Slide 2
Outline
M-X type fuels
NSUF: Argonne National Laboratory
In-situ IR TEM tests
Post-processing analysis
Defect growth model
Fuel Insights
UN vs UO2
Previous studies
Loop types
Loops near the GBs

## Slide 3
Outline
UN as advanced nuclear fuel
Uranium Mononitride: MX-type nuclear fuel
DIMENSIONAL INSTABILITY  POINT DEFECT SINKS
MICROSTRUCTURE
COMPOSITION
Dislocations
(loops, lines)
Grain boundaries
Impurities (thermomechanical processing)
Gas bubbles (at certain sinks: dislocations, GB, impurities)
Cavities (represent swelling)
Fission swelling
Thermal conductivity
Density
Advanced Nuclear Fuel:
Generation IV reactors
  BREST-OD-300
  SVBR-75/100
  BN-800
Thermal propulsion rockets
Li-cooled spaced power reactors
UN defect growth model – Cluster dynamics code CENTIPEDE
Modelling validation & calibration
Sensitivity analysis of diffusion coefficients
Notes: UO2: Is poor conductor with higher thermal gradients (center T 2400oC compared to U- N and C that reach 1400oC)
Irradiation Stability, Chemical compatibility with most of the cladding materials, Longer fuel cycle time owing to neutronic behavior of UN in the core (UO2 18months vs 25 for UN for 50GWd/tU)  Leads to fewer shut-downs for reloading
Swelling is caused by bubbles of fission gas (Xe, Kr), whose evolution is governed by diffusion mechanisms, fuel microstructure,
and irradiation. Breakaway swelling refers to faster bubble growth and increased swelling rate due to irradiation induced changes to the fuel microstructure
Fission gas bubbles that sit on dislocations drive this phenomenon – Fission gas swelling drives breakaway swelling – it is important to develop models that predict dislocation growth characteristics (they also describe fission gas swelling/breakaway swelling) – rely on accurate diffusion coefficients -> those coefficients also dictate dislocation growth so need to validate those
“Breakaway swelling” in UN:
Sudden change in rate of swelling once a threshold temperature is reached (region I II)
As burn-up increases the threshold temperature lowers
UO2: Is poor conductor with higher thermal gradients (center T 2400oC compared to U- N and C that reach 1400oC)
Irradiation Stability, Chemical compatibility with most of the cladding materials, Longer fuel cycle time owing to neutronic behavior of UN in the core (UO2 18months vs 25 for UN for 50GWd/tU)  Leads to fewer shut-downs for reloading
Fission gas bubbles that sit on dislocations drive this phenomenon – Fission gas swelling drives breakaway swelling – it is important to develop models that predict dislocation growth characteristics (they also describe fission gas swelling/breakaway swelling) – rely on accurate diffusion coefficients -> those coefficients also dictate dislocation growth so need to validate those
“Breakaway swelling” in UN:
Sudden change in rate of swelling once a threshold temperature is reached (region I → II)
As burn-up increases the threshold temperature lowers

## Slide 4
Outline
UN as advanced nuclear fuel
UN defect growth model – Cluster dynamics code CENTIPEDE
Modelling validation & calibration
Sensitivity analysis of diffusion coefficients
Breakaway swelling – BISON fuel performance simulation
Differences between ion- and reactor-based irradiations
diffusion coefficients: DU, DN , Dxe
dislocation size and density:
bubble concentration and size
Direct extrapolation
BISON
CENTIPEDE
Test reactor data
Notes: Ion beam is not representative of in reactor conditions –
Utilize controlled experimental parameters to validate the model (Centipede)
Apply established mechanistic parameters into paired model (Bison – Centipede) in order to predict breakaway swelling from radiation damage in-reactor
Reduce uncertainty in-reactor conditions through machine learning
but we validate the same modelling parameters that apply in fuel performance application -> that is why modelling is important. Fission gas swelling drives breakaway swelling – it is important to develop models that predict dislocation growth characteristics (they also describe fission gas swelling/breakaway swelling) – rely on accurate diffusion coefficients -> those coefficients also dictate dislocation growth so need to validate those
Predict breakaway swelling from radiation damage in-reactor & reduce uncertainty in-reactor conditions through machine learning

## Slide 5
Outline
UN as advanced nuclear fuel
RTE proposal–IVEM facility
Rapid Turnaround Experiment proposal:
#1868: Elucidating the Effect of Radiation-Induced Defect Accumulation on Swelling in UN using in-situ TEM Irradiation
Intermediate Voltage Electron Microscope facility

## Slide 6
Outline
UN as advanced nuclear fuel
RTE proposal–IVEM facility
In-situ IR TEM tests
Temperature: 1000 oC
Duration: 34’ 43’’
Total dose: 4.66 dpa
2-beam kinematical condition  zone axis [110], g 200
EDS elemental analysis at room temperature before and after ion irradiation
Oxygen signal is apparent after the irradiation test at 1000 oC
Kosmidou et.al., Temperature dependency of dislocation evolution in Kr-irradiated Uranium Mononitride (UN) through in-situ TEM observation and modeling, Acta Materialia, 2025

## Slide 7
Outline
UN as advanced nuclear fuel
RTE proposal–IVEM facility
In-situ IR TEM tests
Temperature: 1000 oC
Duration: 34’ 43’’
Total dose: 4.66 dpa
Dislocation evolution:
Point defect formation – depletion
Dislocation loop nucleation
Dislocation loop growth
Co-existence of dislocation loops and lines
Tangled network
Area: 785 x 785 nm

## Slide 8
Outline
UN as advanced nuclear fuel
RTE proposal–IVEM facility
In-situ IR TEM tests
Coalescing events
Surface sink
Loop – line interaction

## Slide 9
Outline
UN as advanced nuclear fuel
RTE proposal–IVEM facility
In-situ IR TEM tests
Experimental Integration Defect growth model
Kosmidou et.al., Temperature dependency of dislocation evolution in Kr-irradiated Uranium Mononitride (UN) through in-situ TEM observation and modeling, Acta Materialia, 2025
Notes: The loop size: rapid rise of the loop size as the dose increases. However, due to the broad standard deviation across all the tests and their overlapping nature, there is no significant evidence supporting temperature dependency in loop size. Loop density: a linear trend across all temperatures with lower loop density values observed at higher temperatures.
The rise of loop density at the early stages of ion dose shows their nucleation and growth, reaching the saturation peak for all temperatures below 1 dpa.

## Slide 10
Outline
UN as advanced nuclear fuel
RTE proposal–IVEM facility
In-situ IR TEM tests
Experimental Integration Defect growth model
UN defect growth model – Cluster dynamics code CENTIPEDE
Kosmidou et.al., Temperature dependency of dislocation evolution in Kr-irradiated Uranium Mononitride (UN) through in-situ TEM observation and modeling, Acta Materialia, 2025
Notes: Critical uncertainties
Model formulation: Nucleation and growth by interstitial absorption
Defect energies and diffusivities
Model parameters  Sink bias
The mechanistic model in Centipede can be used to apply the cluster dynamics dislocation model despite the higher dose rate than in-reactor conditions (3 orders of magnitude higher with ions).
In place of a dislocation coalescence model, the experimental concentrations were utilized, with the dislocation sizes solved via the cluster dynamics model.
The comparison between data and the model were reasonable.

## Slide 11
Outline
UN as advanced nuclear fuel
RTE proposal–IVEM facility
In-situ IR TEM tests
Fuel insights
Experimental Integration Defect growth model
Comparative Analysis: UN vs UO2
*
*He et.al., In situ TEM observation of dislocation evolution in Kr-irradiated UO2 single crystal, JNM, 2013
Identical IR conditions:
1MeV Kr2+
800 oC
Flux: 7.70E11 for UO2
6.25E11 for UN
Defect evolution in UN compared to UO2:
↓ loop size and ↓ growth rate
↑ loop density with lower critical dose for loop saturation
Dislocation loop types in fcc
Faulted dislocation loops(≤20nm size) have been observed in CeO2 (IR: 1MeV Kr2+, 800 oC) and in ThO2 (IR: 1MeV Kr2+, 600 oC)
Not observed experimentally in U-based alloy with fluorite structure (e.g. UO2)
CeO2 at 800 oC
IR: 1 MeV of Kr2+
5E14 ions/cm2
*W. Chen et.al., Characterization of dislocation loops in CeO2 irradiated with high energy Kr and Xe, Phil. Mag., 2013
fcc fluorite
*P. Xiu et.al., Dislocation Loops in Proton Irradiated U-N-O System, JNM, 2021
UN at 710 oC
IR: 2 MeV of H+
8E18 ions/cm2
fcc rock-salt
Formation of perfect loops in UN (IR: 1MeV Kr2+, 600-1000 oC)
Faulted dislocation loops (6-10nm) have been observed at 1100 oC
UN at 1100 oC
IR: 1 MeV of Kr++
1.32E15 ions/cm2
Kosmidou et.al., Temperature dependency of dislocation evolution in Kr-irradiated Uranium Mononitride (UN) through in-situ TEM observation and modeling, Acta Materialia, 2025
Notes: Loop size: Rapid rise of loop size as a function of dpa. However, due to the broad st. dev across all tests and their overlapping nature, there’s no significant evidence supporting T dependency in loop size.
Loop density: Linear trend across all T with lower loop density values observed at higher T.

## Slide 12
Outline
UN as advanced nuclear fuel
RTE proposal–IVEM facility
In-situ IR TEM tests
Fuel insights
Experimental Integration Defect growth model
Cavity formation
Dislocation loop formation near GB
Intragranular loops (7-14nm) were observed prior to the irradiation test at 1100 oC
TEM-BF micrographs oriented far from Bragg conditions (under-focus: 1.2 µm of negative defocus) showing the presence small intragranular cavities in UN irradiated at 700, 800, 1000, and 1100 oC
Thermally activated diffusion of point defects from Ga ion impingement
Nanoscale radiation-induced loops preferentially nucleate and grow within a 10 nm width-zone area from the grain boundary. Loop coalescing events are mostly apparent to the left side of the zone and small size near the GB migrate to the sink.
Kosmidou et.al., Temperature dependency of dislocation evolution in Kr-irradiated Uranium Mononitride (UN) through in-situ TEM observation and modeling, Acta Materialia, 2025

## Slide 13
Fuel insights
Summary
Outline
UN as advanced nuclear fuel
RTE proposal–IVEM facility
In-situ IR TEM tests
Experimental Integration Defect growth model
In-situ TEM tests
Evolution of loop size and density as a function of dpa for 700,800,900,1000 oC
Defect growth model
UN vs UO2
Comparative analysis with UO2: ↓ loop size and ↑ loop density
Perfect - faulted loops
Edge-on faulted loops we observed only at 1100 oC.
Cavity formation
No great change in cavity size at different temperatures and doses.
Loops near GB
Intragranular dislocation loops are formed near the GB at 1100 oC (coalesce and migration of loops).
Targeted irradiation tests allow direct validation of dislocation and fission gas behavior predicted by mechanistic swelling model